Quality and Testing Regulations

for Vacuum Insulation Panels - VIP

Version November 2010

Translation February 2016

Güteschutzgemeinschaft

Hartschaum e.V. (GSH)

Schildenstraße 24

29221 Celle

Tel.: (051 41) 88 92 65

Fax: (051 41) 88 92 67

E-mail: info@gsh.eu

Internet: www.gsh.eu

Quality and Testing Regulations for Vacuum Insulation Panels - VIP

# Scope

These Quality and Testing Regulations apply to the production of Vacuum Insulation Panels abbreviated to VIP in the following Quality and Testing Regulations.

VIP is a thermal insulating product which has 5 to 10 time lower insulation thickness then conventional insulation materials with the same heat transfer coefficient. The mostly “plate-shaped” core of VIP consists of nano or microporous or open-pored material. It is shrink-wrapped in an high permeation-tight film and evacuated.

For years, VIP have been used for different applications such as refrigerators and freezers, temperature-controlled packaging, in the cryogenic field, logistic area and in the construction sector. For the construction field the advantage of the space-saving alternative VIP is given for insulating of floor, terrace, flat roof, wall and facade elements.

VIP products for which the quality mark may be used must comply with EN 4102-1, not less than German building material class B2 or Euroclass E.  In addition to this it has to comply with the building approval of the manufacturer in the current valid version and has to fulfil the requirements of these quality and testing regulations.

## Quality Types

The quality mark may only be used for VIP products shown in Table 1

Table 1: VIP Quality types

| Quality type | B | Building and construction industry |
| --- | --- | --- |

## Terms, definitions and abbreviations

DiBt	Deutsches Institut für Bautechnik / German institute for construction engineering

EOTA 	European Organisation for Technical Approvals

WPK	Werkseigene Produktionskontrolle / Factory production control (FPC)

VIP	Vakuum-Isolations-Paneele / Vacuum Insulation Panel

ETZ	Europäische Technische Zulassung / European technical Approval (ETA)

# Normative references

These quality and testing regulations are based on regulations from European and German standards. The full titles of these normative references are listed below. Undated references are used, whereby the last issue of the relevant standard (including all changes) applies. The following documents are required for use in these quality and testing regulations.

DIN EN ISO 11925-2	Reaction to fire tests - Ignitability of products subjected to direct impingement of flame – Part 2: Single-flame source test

DIN 4102-1	Fire behavior of building materials and building components – Part 1 : Building materials, concepts, requirements and tests

DIN EN 10204	Metallic products – Types of inspection documents

DIN EN 12667	Thermal performance of building materials and products

Determination of thermal resistance by means of guarded hot plate and heat flow meter methods

Products of high and medium thermal resistance

DIN EN 822	Thermal insulating product for building applications – Determination of length and width

DIN EN 823	Thermal insulating products for building applications – Determination of thickness

DIN EN 824	Thermal insulating products for building applications – Determination of squareness

DIN EN 825	Thermal insulating products for building applications – Determination of flatness

DIN EN 826	Thermal insulating products for building applications – Determination of compression behaviour

DIN EN 1602	Thermal insulating products for building applications – Determination of the apparent density

# Quality and testing requirements, monitoring

## Area regulated

VIP products have to have a general technical approval (abZ) from DIBt or an European, technical approval (ETZ) of EOTA in order to apply for the quality mark.

## Additional quality requirements

In addition to the respective general building supervisory approvals from the DIBT or ETZ of EOTA for required tests, the requirements under 3.2.1 have to be audited in order to be awarded with the quality mark.

The additional tests must be carried out by a testing body named by the quality committee (Güteausschuss) of the quality assurance group (GSH). As a rule all notified bodies are accepted.

3.2.1	Initial type test and monitoring by the testing body

All quality types for which an application for the RAL Quality Mark has been made are subject to an initial type test in accordance with the approval and product standards.

The pre-requisites for being awarded and allowed to carry the quality mark “Vacuum Insulation Panels – VIP” are that the initial type tests have been passed and an initial inspection of factory production control (FPC) has been carried out. The content of the initial test result from the following regulations. An application for the initial type test is made to the GSH according to the implementing regulations. Within the framework of the initial type test it is to be determined, whether the quality assured Vacuum Insulation Panels - VIP fully meet the requirements laid down in the quality and testing regulations.

Quality and testing conditions

Following criteria are monitored within the initial test :

Thermal conductivity :

- specimen taken in the factory by the inspection body:

- Specimen A : 3 pieces, length 400 – 600 mm (rectangular or square-shaped)

lower thickness-range

- specimen B : 3 pieces, length 200 – 300 mm (rectangular or square-shaped)

lower thickness-range

- specimen C : 2 pieces, length 400 – 600 mm (rectangular or square-shaped)

upper thickness-range

- Provided quantity of testing material : from minimum three different production days, in total three times the amount named above.

The provided testing material is needed for the initial test as stated in table no. 2 :

Table 2 : Allocation of specimens and audits

|  | Specimen A | Specimen B | Specimen C |
| --- | --- | --- | --- |
| Measurement of thermal conductivity | X |  | X |
| Measurement of Water absorption, sorption isotherme |  |  | X |
| Measurement of Internal pressure (before ageing) | X | X | X |
| Ageing at a climate of 23ºC, 50% r.h. for 6 months (depending on shape) | X | X |  |

- Inspection of statistics of production  / Factory production control

- Thermal conductivity test :

  - Measurement  initial value (VIP samples) : 3 thicknesses

  - Characterization / Core material characteristics (of the collected VIP samples)

    - Measured at increased internal pressure (50 – 100 mbar), determination p =  / p,

    - Measured at ambient pressure (ca. 1000 mbar),

    - Measured at increased moisture content XW (Masse-%), determination Xw =  / XW,

- Measurement of the water absorption, Sorptions-Isotherme XW():

  - Drying at 105°, compensation moisture balance of ca. 30 % r.h. und ca. 60 % r.h.

- Measurement of the internal pressure (before ageing)

- Ageing at a climate of  23°C, 50 % r.h., 6 months:

  - 2 × 3 specimen (lower thickness range, 2 sizes),

  - Yearly increase of the internal pressure pa, water content XWa,

  - Determination of the dependency of size.

- Determination of the long-term value see formula below :

(t)	= 0 + p × pa × t + Xw × XW,eq × (1 – e(-t /))

whereby

0	 = 90 % fractile value factory statistics (none aged), minimum 10 test values [W/(m·K)]

P      =	pressure dependent increase of thermal conductivity [W/(m·K))/mbar]

pa	    = yearly increase of the inner pressure of VIP [mbar/a]

t	   = time	[a]

Xw	= increase of thermal conductivity caused by moisture [W/(m·K))/Mass%]

XW,eq	=	compensation moisture balance content 23°C, 50 % r.h. [Mass%]

=	XW,eq / XWa, time constant compensation moisture balance [Mass% (Mass/a)]

(t) for t = 25 years, depending on size  [W/(m·K)]

Monitoring is carried out to determine whether the applicant fulfils the requirements for proper compliance with the quality and testing regulations. The applicant is obliged to present existing records of the FPC to the monitoring body if requested to do so.

With successful passing of the first test and the FPC monitoring the first monitoring test is done.

3.2.2 Factory  production control (FPC), (self-monitoring)

Every owner of the quality mark has to carry out a factory production control (FPC) for all quality assured VIPs according to the quality and testing regulations and needs to document the results  in writing. This documentation of the factory production control needs to be kept for minimum 10 years and to be handed to the inspection body if desired.

During the FPC following properties have to be monitored and documented :

- source materials of barrier, core material etc. according to  raw-material specification and certificate of compliance     with the order according to DIN EN 10204:2.1 → receiving inspection

- Length, width (without folded envelope)

→ daily

- Thickness       (without folded envelope)

→ daily

- Apparent density    (core material)

→ daily

- Flatness

→ daily

- Thermal conductivity, measured directly after production according to test method specified by the Quality Committee. The device used for the thermal conductivity during the FPC has to be calibrated once a year.

→ daily

- internal pressure :

- (1) minimum frequency of control per day :

- 1 when less than 10 pcs. daily production

- every 10th panel when 10-100 pcs. daily production

- 10 when more than 100 pcs. of daily production

- (2) after occurrence of an error (inner pressure > 5 mbar) :

- ongoing individual control up to 70 pcs. If no error occurs one can return to the test frequency (1).

Otherwise the circumstances of error have to be clarified and corrected. Than a new ongoing individual

Control takes place, again up to 70 pcs. except for obviously damaged VIP.

- (3) the annual statistics have to show a measured error frequency of < 1%.

- Compressive stress at 10% compression or compressive strength

→ once a week

- Ageing :

- Storage from retention samples from the production at interior climate conditions, storage for at least 12 months.

→ once a month

- Measurement of the inner pressure before and after storage

3.2.3	External control

External control ensures that the user of the quality mark complies with the requirements of these Quality and Testing Regulations. The content and frequency of testing is defined in the general building approval. The monitoring is based on these quality and test regulations. Within the framework of the external control, VIPs  are randomly taken and examined.  The test results are submitted to the GSH for evaluation.

The testing properties for the external monitoring are :

- Length, width (without folded envelope)

- Thickness      (without folded envelope)

- Apparent density   (core material)

- Thermal conductivity (after delivery and with increased inner pressure from 50-100 mbar)

- Increase of internal pressure :

- Measurement of provided samples from manufacturer including reference to date of production and of initial value of the inner pressure.

One test result has to be performed for every property.

3.2.4    Monitoring reports and their retention period

All documents associated with the RAL Quality Mark must be retained for at least 10 years

# Marking and labelling

## Quality mark

VIP products which comply to these Quality and Testing Regulations are to be marked with the quality mark shown below:

The Quality Mark is registered as a trademark with the German patent and trademark office.

Solely the implementing regulations for the award and use of the quality mark VIP apply for the use of the quality mark.

## Labels

Above and beyond the marking rules regulated in the Approval, the quality assurance types listed in clause 1.1. are to be included on the labels as further identification features.

# Changes

Changes to these Quality and Testing Regulations, including editorial changes, require the prior approval of RAL in order to become effective. They come into effect within an appropriate period after they have been announced to the user of the quality mark.

Implementing regulations for the award and use of the

quality mark VIP Vacuum-Insulation-Panel

1 Quality principle

The quality principle for the quality mark consists of the quality and testing regulations for Vacuum-Insolation-Panels. They are added to and developed in line with the technical progress.

2 Award

2.1 On application, Güteschutzgemeinschaft Hartschaum e. V. awards companies the right to carry the quality mark of the quality assurance group.

2.2 The application is to be addressed to the office of Güteschutzgemeinschaft Hartschaum e.V. in writing. A signed, legally binding Certificate of Commitment (Template 1) is to be enclosed with the application.

2.3 The application is checked by the Quality Committee. The Quality Committee inspects the applicant’s products without pre-announcement according to the Quality and Testing Regulations. It can visit the applicant’s company, inspect the applicant’s products to determine whether they comply with the quality and testing regulations and request and view the documents mentioned in the quality principle. It issues a report on the results of the inspection and sends this to the applicant and the Chairman of the Quality Assurance Group. The Quality Committee can entrust sworn experts or a state-recognized testing body with these tasks. Before beginning the audit the person entrusted with the task must present its authorization. The costs are paid by the applicant.

2.4 If the audit is passed, the board of the Quality Assurance Group at the suggestion of the Quality Committee awards the applicant the quality mark. The award is certified (Template 2). If the audit is failed, the Quality Committee rejects the application. It must give reasons in writing for this rejection.

3. Use

3.1 Users of the quality mark may only do so for products which comply with the quality and testing regulations.

3.2 Only the Quality Assurance Group is entitled to have means of marking related to the quality mark (metal embossing, embossing tools, printed material, lead seals, seal mark, rubber stamp, and the like) produced and to issue these or have these issued to the user of the quality mark and to specify precisely the type of use.

3.3 The board can issue special regulations for the use of the quality mark in advertising and in joint advertising in order to ensure the integrity of competition and prevent misuse of the mark. This must not hinder individual advertising. Here applies the same maxim of the integrity of competition.

3.4 If the right to use the quality mark has been legally withdrawn, the award certificate and all means of marking related to the quality mark are to be returned; a right to a refund does not exist. The same applies if the right to use the quality mark has expired by other means.

4. Monitoring

4.1 Güteschutzgemeinschaft Hartschaum e.V. is entitled and obliged to monitor the use of the quality mark and the compliance with the quality and testing regulations. Evidence of the continuity of monitoring is to be presented to RAL in the form of a monitoring contract with a neutral testing body or authorized auditor.

4.2 Each user of the quality mark is responsible for ensuring that it complies with the Quality and Testing Regulations. It is its duty to carry out continuous quality control. It must record the factory production control carefully. The Quality Committee or its authorized representatives can view the records at any time. The user of the quality mark subjects its quality assured products to monitoring tests by the quality committee or its representative to the extent and in the frequency appropriate for the requirements of the Quality and Testing Regulations. It pays the costs of testing.

4.3 Auditors can inspect and view quality assured products in the quality mark user’s company at any time during operating hours.

4.4 If the result of a test is negative or if fault is found with a product / service, the Quality Committee orders that the test is to be repeated.

4.5 A report on each test result is to be issued by the testing body commissioned. The Quality Assurance Group and the user of the quality mark each receive a copy of this.

4.6 If criticism of a product proves wrong, the party making the criticism bears the costs of the test; if it proves right the quality mark user has to bear the costs.

5 Punishment of violations

5.1 If the Quality Committee detects faults in the quality assurance, it suggests punishment measures to the board of the Güteschutzgemeinschaft Hartschaum e.V. These  depend on the gravity of violation :

5.1.1 additional tasks within the framework of the FPC,

5.1.2 increase of the external tests,

5.1.3 warning,

5.1.4 contractual penalty up to the amount of € 2.000,

5.1.5 temporary or permanent withdrawal of the quality mark,

5.2 users of the quality mark who violate against paragraphes 3 or 4 may receive a warning.

5.3 Instead of a warning a contractual penalty can be imposed up to € 2000,- for each individual case. The contractual penalty has to be paid to Güteschutzgemeinschaft Hartschaum e.V. within 14 days after the notification has become legally binding.

5.4 The measures mentioned in Section 5.1 can be combined with each other.

5.5 Users of the quality mark, wo repeatedly violence against Section 3 or 4 are sanctioned with the permanent or temporary withdrawal of the quality mark. The same applies for users of the quality mark who delay or hinder the tests.

5.6 The affected party shall be given a hearing before any actions are imposed.

5.7 The penalties described in sub-section 5.1-5.5 take effect as soon as they legally come into force.

5.8 In urgent cases the chairman of Güteschutzgemeinschaft Hartschaum e.V. may withdraw the quality mark temporarily with immediate effect. Such action must be confirmed by the board of Güteschutzgemeinschaft within 14 days.

6 Complaints

6.1 The user of the quality mark may complain to the quality committee about notification of punishment within 4 weeks after it has been delivered.

6.2 If the Quality Committee rejects the complaint, the claimant may take legal action in accordance with clause 17 of the statutes of Güteschutzgemeinschaft Hartschaum e.V. within 4 weeks after notification has been delivered.

7 Re-award

If the right to use the quality mark has been withdrawn, it can be re-awarded after three months at the earliest. The procedure described in clause 2 of these implementing regulations is followed. However, the board of Güteschutzgemeinschaft Hartschaum e.V. may impose additional conditions.

8 Changes

These implementing regulations and the specimens (certificate of commitment, certificate of award) are recognized by RAL. Changes, including editorial changes, must be approved in writing by RAL before they become effective. Changes become effective within an appropriate period after they have been announced by the board of  Güteschutzgemeinschaft Hartschaum e.V..